SESSION 5 -COOKING UTENSILS
(Capacity Building Programme for Women and Child Welfare)

Indian Standards Covered: -

- IS 14756 – Stainless Steel Utensils

- IS 1660 – Wrought and Cast Aluminium Utensils

- IS 2347 – Domestic Pressure Cooker

- IS 17870 – Commercial Pressure Cooker

- IS 17693 –  Non-electric Cooling Cabinet Made of Clay (Mitticool Refrigerator)

Existing Regulations:

- Domestic pressure cookers are under mandatory certification (390 BIS licensees)

- DPIIT, Ministry of Commerce and Industry, mandates certification for cooking utensils with following implementation dates depending upon the category of enterprises:

| Sl No | IS No | Title of the Indian Standard | Last date of implementation for large scale enterprises | Last date of implementation for micro scale enterprises | Last date of implementation for small scale enterprises |
| --- | --- | --- | --- | --- | --- |
| 1 | IS 14756: 2024 | Stainless Steel Utensils | 1st April, 2025 | 1st October, 2025 | 1st July, 2025 |
| 2 | IS 1660: 2024 | Wrought and Cast Aluminum Utensils |  |  |  |

### Health Hazards:

- Sometimes, there is possibility of migration of material from cooking utensils to the food being cooked.

- To take care of this issue, standardization plays an important role.

- Standards prescribe the performance and safety requirements to ensure that product is of robust and durable nature.

- Most importantly, these standards prescribe the permissible limits of heavy metals or toxic materials in the raw materials used in manufacturing of Utensils.

- IS 14756: 2024 : Stainless Steel Utensils

- Scope: Covers cooking, serving, table, and storage utensils.

- Material Requirements:

- The stainless steel used for manufacture of utensils shall conform to IS 5522 (Stainless steel sheets and strips for utensils) or IS 15997 (Low nickel austenitic stainless-steel plate, sheet, and strip for utensils and kitchen appliances).

- The material used for composite bottom shall be as per IS 15960 (Composite bottom stainless steel cooking utensils).

- If the body of the utensil is made of a 3 ply construction, 3 ply material shall be made with inner layer – designation X04Cr19Ni9 (grade 304) of IS 5522, middle layer – aluminium as per IS 21 and outer layer – designation X07Cr17 (grade 430)/X02Cr18Ti (grade 439) of IS 6911 (Stainless steel plate, sheet and strip)

- Performance Tests:

- Staining Tests: the utensil shall not show any sign of staining after removal from the test solutions/conditions.

- Mechanical and Thermal Shock Test (for cladded utensils only): the cladded or deposited layer shall show no sign of peeling off or coming off.

- Dry Heat Test (for cladded utensils only): There shall be no separation of cowl or disc from the utensil after cooling.

- Nominal Capacity Test: The nominal capacity of cookware shall be expressed only in complete or 100 ml units. No negative tolerances shall be allowed on the nominal capacity.

- Tempered Glass Lid (Thermal Shock Test): glass lid in air circulating oven (120 deg Celsius for 30 mins); after removal the glass lid shall not shatter when pouring one litre of water at ambient temperature.

- Tempered Glass Lid (Free Fall Test): Drop the lid with/without rim facing down, from a height of 900 mm on a vitrified tile surface or a level smooth concrete surface. The glass shall not break/crack.

- IS 1660: Wrought and Cast Aluminium Utensils

- Scope: Covers the commonly used wrought and cast aluminium utensils upto 30 litres capacity

- Material Requirements:

| Utensils and its various body parts | Relevant Complying Indian Standard | Additional Requirements |
| --- | --- | --- |
| Main body of utensil, strips | IS 21 / IS 737 : Wrought aluminium and aluminium alloy sheet and strip for general engg. purposes | Toxic metals (Pb, Cd, Hg, Cr(VI)) – 0.05% (max) |
| Cast Cookware | IS 617 : Aluminium and aluminium alloy ingots for remelting & castings(general engg. Purposes) | _ |
| Other aluminium components and parts | IS 737 / IS 617 / IS 734 (Specification for wrought aluminium and aluminium alloy forging stock and forgings) | _ |
| Lids (if provided), SS handles, rivets and fittings | IS 21 / 737 (Aluminium), IS 6911 / IS 5522 (SS) | Minimum thickness of SS lid is 0.4 mm; if tempered glass lid 3.5mm (min thickness) |
| Gasket (if used) | _ | Made from food grade silicon/nitrile |
| Lunch box clips | Aluminium alloy wire – IS 739 (19000 Designation) | _ |

- Major Performances Tests:

- Handles: Should be sturdy and strong enough to withstand the weight.

- Coating: Requirement of PTFE, ceramic coating, powder coating and high temperature resistant liquid coating is that the material shall not contain more than 0.05 percent as metal of any toxic metals such as lead, cadmium, mercury or chromium(VI).

- Lunch Box Performance Test: snapping the clip on and off for 2000 times; no weakening or damage to the securing arrangement shall be observed.

- Ground Nut Oil Test for Leakage: filling inner pot of box by two third ground nut oil and then inverted; no appreciable leakage of the oil from the inner pot shall occur after one minute.

- Tempered Glass Lid (Thermal Shock Test): glass lid in air circulating oven (120 deg Celsius for 30 mins); after removal the glass lid shall not shatter when pouring one litre of water at ambient temperature.

- IS 2347: Domestic Pressure Cooker

- Scope: Covers the requirements for domestic pressure cookers upto 24 litres.

- Material Requirements:

- Body, Lid, Containers and Grid — The body and lid of the pressure cooker shall conform to designation 19000, 19500, 31000, 40800 of IS 21 or stainless steel conforming to designation X04Cr19Ni9/X07Cr18Ni9 of IS 5522/IS 6911 or stainless steel conforming to designation X8Cr16Mn8Cu2Ni2N of IS 15997/IS 6911. The containers and the grid shall conform to any of the designations as per IS 21 or IS 5522 or IS 15997.

- If stainless steel pressure cooker is provided with composite bottom, the composite bottom shall conform to IS 15960.

- If the aluminium cooker is provided with an induction friendly base, the material of the induction plate shall be as per 430 or 439 series as given in IS 6911.

- If the body of the pressure cooker is made of a 3 ply construction, 3 ply material shall be made with inner layer grade 304 of IS 5522, middle layer – aluminium as per IS 21 and induction friendly outer layer – grade 430 /439 of IS 6911.

- Performance Tests:

- Air pressure test

- Proof pressure test

- Operating test for pressure regulating device

- Bursting pressure test

- Lid Opening Test for outer lid and inner lid cooker

- IS 17870: Commercial Pressure Cooker

- For cookers above 24 liters and up to 100 liters.

- Maintains nominal cooking steam pressure of 0.8 kgf/cm².

- Material and performance requirements are similar to IS 2347

- IS 17693 –  Non-electric Cooling Cabinet Made of Clay (Mitticool Refrigerator)

- Scope: Covers the requirements of a cooling cabinet made out of clay which is also called mitticool refrigerator.

- Special Application:

- This product works on the same principle as that of earthen pots which are used to cool water in summer which means the inside cabinet temperature, not below the ambient wet-bulb temperature can be maintained.

- useful for areas where electrical power is not available.

- not suitable to preserve the foodstuff which are required to be stored in frozen state.

- Requirements:

- Construction: Main body is constructed with clay. Door may be metallic or non-metallic which is fixed on the cabinet with stainless steel hinges conforming to IS 12817 or similar non-corrosive material. Chrome plated tap shall be used to draw water from the cabinet.

- Cooling Performance: At defined steady-state condition, cooling performance is measured by comparing ambient DBT (dry-bulb temperature) and the cabinet internal DBT.

- Volume: The method to determine cabinet volume is also defined.

- User manual is provided with the product indicating the type of food stuff which can be stored in it along with time period.

### Other Standards on Consumer Goods for Household Use:

- Electrical Appliances: IS 374, 366, 1293, etc.

- Bathroom Products: IS 12701, 8931, etc.

- Furniture and Fittings: IS 1341, 12817, etc.

- Medical Products: IS 3055, 16289.

- Products for Women and Children: IS 17509, 17514.

- General Utility Products: IS 15558, 1610, etc.